Brittle fracture

of a body with an initial crack

LEFM - linear elastic fracture mechanics

Basic concepts:

Crack

Nucleation (initiation) site

Crack front

Crack tip

Fracture area

Phases of the fracture process:

1. Nucleation phase

Initiation of a macroscopic crack

2. Stable crack propagation

Critical crack length, failure by a leakage

3. Unstable crack propagation

Fracture (fatigue)

Discontinuity vector δ

characterizing the deformation in the crack front surroundings

Zero opening 			MODE I (opening)

MODE II (in-plane shear)			MODE III (out-of-plane shear)

Linear elastic fracture mechanics (LEFM)

Generalization of the equations

K-conception

is based on the basic quantity for crack behaviour description, which is called

stress intensity factor (K-factor)

K-factor can determine

- Dimensions of the plastic zone

- Shape of the opened crack

- Crack driving force  - strain energy released by the crack propagation

Shape of the opened crack

Dependence of the ultimate K-factor value

on the component thickness (type of stress state)

plane stress state

plane strain state

KCI=KIC = fracture toughness

Example of the dependence of fracture toughness on temperature

Examples of formulas for K-factor calculation

Algorithm of the solution of a body with a crack

- Determination of the crack size

- Calculation of K-factors

- Comparison of K-factor values for the individual modes

- Determination of material characteristics (yield stress σy, fracture toughness KIC)

- Determination of the plastic zone radius rk

- Estimation of LEFM applicability

- Comparison of the  KI  and  KIC  values.

In the case of cyclic loading, the following additional steps can be carried out:

- Calculation of the critical crack length  ac

ac=KICσ2.1π

This formula is valid approximately between for Kath≤Ka≤KIC(stable crack propagation).

9.	Estimation of the residual lifetime of the body with the crack

stable crack propagation

unstable crack propagation

Stable crack propagation under conditions of high cycle fatigue

The crack growth rate vT depends on the stress intensity factor KI. Between its threshold value Kath and the fracture toughness KIC this dependency (see fig.173) can be described by a linear relation (in logarithmic coordinates), which gives (after mathematical removal of logaritms) the following exponencial relation (called Paris-Erdogan formula):

dadN=cΔKIm

Here the constants c,m depend on the material and the loading cycle character. The allowable number of cycles can then be calculated by integration of this formula:

ΔN=2af1−m2−a01−m2cΔσmπm22−m

where ΔN represents the number of cycles before the crack achieves its critical (or allowable) length ac (af= ac/FOS), when starting from the initial crack length a0. Stress range Δσ = 2σa corresponding to the stress intensity factor range ΔKI is used here.